### Material Testing of Sneakers

### Objectives

- Conduct compression tests on a sample of shoe sole material

- Determine the modulus of elasticity of shoe sole material

- Determine the effectiveness of sneaker materials

Introduction

Rubber soled shoes were first marketed as “sneakers” in 19171.  Since then their manufacture has become a matter of both science and fashion.   The role of engineering in the evolution of today’s sneakers has been vital to the innovations made in comfort and utility.  Modern running sneakers are the ultimate culmination of engineering and sports performance.

The purpose of this laboratory experiment is to determine the effectiveness of running shoes as shock absorbers for the human body.  In the lab, the Modulus of Elasticity of the shoe’s soles will be determined, and Stress-Strain plots will be generated using methods that are used to determine the properties of elastomeric materials.  By performing this experiment, you should obtain a better understanding of forces, compression, stress, strain, and mechanical properties of material.

Background

Elastomers

An elastomer is any material that behaves like a rubber under specific conditions2.  The material must be able to be deformed, either by stretching or compressing it, and return back to its original size after the force is removed.  Elastomers also become harder to deform as both the deformation and rate of deformation increase.

The tissues of the body exhibit many different types of elastomeric properties.  One has to make the body tissues more rubbery to use them well.  Ligaments will get shorter with lack of use, thus stretching before exercise where larger ranges of motion are needed is crucial for healthy workouts.  The foot is supported by 25 bones and is connected only by ligaments, and is elastomeric.  The amazing thing about the foot is that it has greater than a 50% energy loss when impacted3.  This means that when your running you only feel about half of the force that your foot experiences on each stride, due to the foots elastomeric properties.

Elastomers used in sports equipment play a very important role in protecting the body.  The primary use of elastomers in equipment involves protection against excessive compression or bending in the body.   Perhaps the best example of elastomers protecting against compression is in the use of running shoes3.

Running Shoes

Even though the shoe is only on the foot it can affect the whole body.  The foot transmits forces and feelings to the entire body.  Start with the bottom of the foot, the heel strikes first, then the whole foot, then the forefoot.

Understanding the materials shoe companies are using to build shoes can help you to better select a shoe based on fit and durability.  Running shoes are made up of three basic components: the outsole, the midsole and upper4.   Each of these components can be made of materials that vary greatly in weight and density.  As these components are put together to construct a running shoe, there’s a wide range of durability factors.  The outsole can vary by type of rubber used and the brand.

Shoe Materials

There are two main types of outsole rubber used in running shoes:  carbon and blown.  Blown rubber because air is injected into the rubber compound for a softer, lighter outsole.  Blown rubber is most commonly used in the forefoot because it’s more flexible, cushier and softer.    The downside of blown rubber is not nearly as durable as carbon rubber which is heavier and harder.  Carbon rubber is used most commonly in the high wear areas of the rearfoot.  Some companies have developed new outsole concepts such as DuoSole from Asics by mixing blown and carbon rubber to get a smooth, yet durable outsole like EFR from Adidas4.

Midsoles are the key to any shoe, due to the importance of its durability3.  There are two main midsole foams: ethylene vinyl acetate (EVA) and polyurethane (PU).  EVA is sponge-like foam that is soft and relatively light, but lacks durability.  Polyurethane is heavier, denser, and more durable and when molded, it creates a firm outer shell creating good stability in the midsole.  However, runners tend to prefer the lighter, softer EVA.

Force and Axial Loading

Force is the energy exerted on an object.  It is defined as the pressure, in pounds per square inch, exerted on a certain area multiplied by that area, in square inches.  Hence, the force is applied to a single point.  Axial loading is the act of applying a force to an object’s axis, where it will be put into tension or compression.

Consider the above figure.  The force, F, is applied in an axial direction subjecting the object to a compressive deformation.

Stress

Stress is defined as the force exerted on an object per unit surface area.  Stress, denoted by the Greek letter sigma, , can be calculated by dividing the force by the surface area of the object  (Equation 1).

(1)

Where

Strain

Strain is defined as the deformation per unit length of an object subjected to a force (Figure 2).  In the drawing below the compressive force causes the object to shorten.  This deformation can be used to calculate the strain.

In Figure 2, the dashed line represents the original length of the object.  When subjected to the load, F, it shortens by a certain magnitude, denoted by the Greek letter delta,  The strain, denoted by the Greek letter epsilon, , is calculated by dividing the magnitude of deformation by the original length of the object  (Equation 2).

(2)

Young’s Modulus

Young’s Modulus (a.k.a Modulus of Elasticity) is a physical property of a material.  It is used to describe the stiffness of materials and the ability of a material to resist deformation.  Elastomers, which are soft, have a much lower Young’s modulus than metals, such as steel, which are very stiff.  Using the plots of stress vs. strain you will be able to calculate Young’s Modulus of Elasticity.   According to literature values, elastic fibers in the body have a Young’s Modulus value of about 0.6 MPa5.

Hooke’s Law

Hooke’s law relates stress and strain by the Young’s Modulus

(3)

Substituting equations 1 and 2 into equation 3, force, displacement and modulus can be related.

The magnitude of deformation (displacement) can be calculated by using Equation 4.

(4)

In this lab you will be using the MTS Universal Elastomer System in order to apply a force to a sneaker sole and measure the stress and strain experienced by the sole.  Using stress verse strain plots will allow you to see a measure of the force absorption properties of the sneaker.

##### MTS Elastomer Procedure

# PreTesting Procedure

- Find the area of the heel press. Trace the heel piece on to a piece of paper, find the area using the tracing. (Hint: To find the area divide the heel shape into a circle and a rectangle.)

- Measure the height of the sneaker.

- Record make of shoe and shoe model.

- Turn on the MTS machine by turning the red knob located on the left face of the Hydraulic Power Unit Control to the on position.

- To the left of the knob is a vertical series of function lights.  The only light that should be illuminated is the green Power On button.  If any other light is on, press the blue Reset button located at the far right of the function lights.

# Testing Procedure

- From the desktop, click on the Station Manager icon.

- Within the configuration folder highlight setupjk.cfg and from the parameters box at the bottom of the open window choose shoe test.  Press Okay.

- The Basic Testware display should appear. (If the Function Generator appears instead, click on the Basic Testware icon on the top toolbar.)

- In the center of the screen is the Master Span panel.  If the small bars next to Interlock and Program are red, click on the gray bars until the lights disappear.

- Activate the hydraulic power supply by clicking on the middle set of bars next to HPS1.  This is low power setting.  Before proceeding to the high power setting, check that the hoses attached to the bottom right face of the Hydraulic Power Unit Control for leaks.  If there are no problems proceed by clicking on the high power setting.

- Enable the software by clicking the low and then high power panels next to HSM1.

- Place shoe sample on the MTS bottom actuator.

- From the Cross Head Lift/Lock Control panel, located next to the Hydraulic Power Unit control, unlock the crosshead by turning the knob on the right of the panel to the unlock position (turning left).

- Move the shaft to about an inch above the shoe sample by turning the bar at the left of the panel down.  Note:  There is no speed control used in moving the top shaft, so be careful.

- Once the top shaft is in the proper position, be sure to return the shaft to the locked position by turning the bar to its original position.

- From the Basic Testware display, click on the Manual Command icon, under the Stations Control.  On the Manual Command screen, check the box at the bottom left corner to enable manual control.

- On the task bar at the bottom of the screen click on the Meters icon and arrange the window so that you are able to see both the Meters window and the Manual Command window.

- Record the initial Axial Force from the Meters window.

- Now move the bottom actuator so that the shoe is in contact with the top actuator by clicking on the arrows in the Manual Command screen.  Move the actuator down (in the negative direction) to 20-30 lbf more than the initial Axial Force.  Have one team member make certain that the shoe is making good contact with the heel press.

- Record the new starting position from the Manual Command window. (ex. –0.2394)

- Once in position, disable the Manual Command by un-clicking the box at the bottom left of the window.

- Subtract 0.075 from the starting position value to obtain the oscillating point.  Enter this value into the Target Setpoint. Make certain that the amplitude value reads 0.075 and the frequency reads 1 Hz.

- Now setup a separate data file by clicking on the Test Setup/Data File icon at the top of the screen.  For these exercises, data files need to be saved under D:users/kadlowec/your team name.  Press Okay and go back to the Basic Testware window.

- Select the Reset/Override button.

- You are now ready to run the tests.  Press the sample run icon and run for 5 cycles then press stop.

- Retrieve the saved data from the D drive and save to a disk for manipulation.  (Ensure that there is enough room on the disk because the file is big.)

##### Calculations

- Open excel

- Open your team’s file

- Save the file to your disk as an “.xls” file

- Load up the saved excel sheet

- Note, the MTS has collected a lot of data.

- Put the data in terms of absolute values

- Have your axial displacement and axial force start at the origin (0,0).  This can be done by taking the initial start value and subtracting it from itself as well as every other value in the column.

- With the data, graph axial force (y-axis) vs. axial displacement (x-axis)

- When graphing use one cycle (the last cycle) of data. There should be five sets total.

- To plot Force vs. Displacement:

  - Click the chart wizard button

  - Choose XY (Scatter)

- Return to the excel spreadsheet and create two new columns; one titled “stress” and the other “strain”

- Calculate values into the excel spreadsheet by using equation (1) for stress and (3) for strain

- Go back to the excel sheet to plot Stress (y-axis) vs. Strain (x-axis), again do not use the first data set.

- The graph should look something like Figure 3

- Select two points and determine Young’s Modulus of the sneaker by using equation 2, the slope of the line is Young’s Modulus.

### Follow-up Questions

- Look up the shoe that you tested on the internet and find the special engineering properties of that shoe.

- What is “pronation”? And how are shoes designed to correct this condition?

- What happens to a shoe’s properties as the shoe ages?

- Look up the modulus of elasticity for other materials you are familiar with (steel, wood, rubber).  Compare the modulus of each of these materials with the modulus of the shoe material.

- Two people of different weight 100 lbs and 200 lbs wear the same size and type of shoe.  One says “the shoes are hard” (i.e. high modulus) and one says “these shoes are soft” (low modulus).  Which person said which statement?  Explain. (Hint – curve fit the data to get an equation relating stress and strain, remember the modulus is the slope (derivative) of the curve.)

##### References

- Mitchell, H. The Modern Athletic Shoe. www.inventors.about.com  May 1997.

- Beer, Ferdinand. Mechanics of Materials.  W.C.B. McGraw Hill, New York: 1992.

- Misevich, Kenneth W.  Elastomeric properties needed in various athletic equipment. May 1987.

- Choosing the right shoe.  Rodale Publishing, www.runnersworld.com.  1999.

- Bu Park, Joon. Biomaterial Science and Engineering. Plenum Press, New York, 1984.

# Text boxes

Figure 2:  Strain on a Block

Figure 1:  Axial Force