PROPERTIES OF ACRYLIC

Acrylic State: multipolymer Application: molding and extrusion compounds Material Properties Mechanical Properties Conditions State 1 State 2 ASTM Elastic Modulus (MPa) 2070 - 2967 tensile D638 Flexural Modulus (MPa) 2001 - 2760 23 ºC D790 Tensile Strength (MPa) 38 - 57 at break D638 Compressive Strength (MPa) at yield or break 52 - 80 D695 Flexural Strength (MPa) at yield or break 63 - 90 D790 Elongation at break (%) 5 - 28 D638 Hardness 22 - 56 Rockwell D638 Izod Impact (J/cm of notch) 1/8" thick specimen unless noted 0.5 - 1.3 D256A Thermal Properties Conditions Pressure State ASTM Coef of Thermal Expansion (10-6/ºC) 44 - 50 D696 Deflection Temperature (ºC) 83 - 90 1.82 MPa D648 Thermal Conductivity (W/m-ºC) 0.222 C177 Physical & Electrical Properties Conditions State ASTM Specific Gravity 1.11 - 1.12 D792 Water Absorption (% weight increase) 0.3 after 24 hrs D570 Processing Properties Conditions Type ASTM Melt Flow (gm/10 min) 2 - 14 D1238 Melting Temperature (ºC) 80 - 105 Tg, amorphous Processing Temperature (ºC) 205 - 260 injection molding 194 - 244 extrusion Molding Pressure (MPa) 35 - 138 Linear Mold Shrinkage (cm/cm) 0.004 - 0.008 D955

Reference: http://www.efunda.com/materials/polymers/properties/

Optical Properties of Plastics

Light Transmission

Plastics differ in their ability to transmit light.  Some plastics are transparent, exhibiting optical properties similar to glass.  Other plastics are opaque, and do not allow any light to pass through.  Translucent plastics allow some light to pass through them, but the images are cloudy and unfocused.  Lastly, some plastics are semi-opaque, allowing enough light to pass through them to be able to make out shadows and vague outlines.  Since the boundaries between these different light transmission values are unclear, there are some rules of thumb.  If a newspaper is placed on the other side of the plastic, and it can be easily read, the plastic is transparent.  If it is cloudy and cannot be read, but general shapes can be distinguished, then the plastic is translucent.  If only vague shadows can be discerned, the plastic is semi-opaque.  If no light is transmitted, the plastic is opaque.

Some plastics used for their transparency properties are acrylic, polycarbonate, and polystyrene.  Some examples of parts are plastic lenses for eyeglasses, bullet proof glass, and automobile headlight assemblies.  Unlike glass, extended exposure to UV light degrades the polymers, causing plastics to yellow and become cloudy.

The polymer crystallinity of the plastic plays a major role in determining the optical properties of plastic.  In a highly crystalline polymer like high density polyethylene and polypropylene, the polymers fold up and form orderly crystals at the plastic solidifies after being melted.  These polymer crystals are approximately the same size as the wavelength of visible light, causing the light to scatter.  As a crystalline material is melted, if does not have any fillers that will scatter light, it will change from opaque to transparent because the crystalline structure disappears.  Amorphous polymers, like acrylic, polycarbonate, and polystyrene do not form crystals; they are naturally transparent.  In general, transparent polymers are noncrystalline and translucent polymers are crystalline.  This not the case in crystalline PET (soda bottles), which is transparent because the crystal size is not visible light's wavelength.  Fillers and additives will usually decrease the light transmission of a plastic.

Index of Refraction

The index of refraction is a measure is how much light bends when it hits an object.  If the object has in index of refraction near that of air, the object will be transparent.  Glass, polycarbonate, polystyrene, and acrylic all have indices of refraction close to air.  When making transparent parts, designers must be careful to keep materials with the same index of refraction together, or else the light will bend in different direction and distort the image.

Acrylic is 17 times stronger than glass and will flex instead of shatter. This makes it virtually childproof. Because the seams are stronger and the aquarium is more flexible, you can count on having an acrylic aquarium longer. It's also clearer than glass, and is a better insulator than glass, which means it takes less energy to heat the aquarium. Acrylic weighs half as much as glass, and the bent corners and fewer seams on an acrylic aquarium adds a sleek design to the tank.

One drawback of acrylic aquariums is the tendency for scratches. However, scratches can be removed or lightened from acrylic whereas it is impossible to remove a scratch from glass. Because acrylic aquariums can scratch easily, only those scrubbers that indicate "can be used on acrylic" should be used. Never use an ammonia product when cleaning the outside of an acrylic aquarium because ammonia will crystallize acrylic. Use only a vinegar and water solution for cleaning the outside of an acrylic aquarium.

Because of their design, acrylic aquariums typically come with a full hood and fluorescent fixture that matches the particular aquarium. Therefore, when comparing acrylic aquariums to glass aquariums, remember to figure in the cost of the hood and light if you are considering a glass unit.